## PART 1: GENERAL

  - INTRODUCTION

Supply and fix Luxalon® Exterior 300L Carrier Ceiling system as manufactured by Hunter Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of panels fixed to a rigid and levelled suspension system which allows for all individual panels to be removed by hand or by using a basic flat bladed tool. The suspension system consist of a non Luxalon® supporting system. To prevent contact corrosion by applying dissimilar metals each fixing of the carrier to the sub-construction must be made through the Luxalon® washer set.

## PART 2: PRODUCT

_________m² Luxalon® 300L Wide Panel Exterior Carrier Ceiling consisting of:

2.1 PANELS

Panels to be roll formed from 0.7 mm thick stove enamelled aluminium strip. The 29 mm high up stands at the panel ends to give enhanced rigidity. The 300 mm wide panels feature square edges to form visually closed joints.

Panels to be manufactured from pre-painted, stove enamelled, alloy EN-AW 3005 or equivalent (according to EN 1396 and ECCA). Panels to have a length of _________ mm (manufacturer availability 1000-6000 mm and on request 250-1000 mm and > 6000 mm).

2.2 SUSPENSION

Rows of 0.95 Alu roll formed carriers shall be installed at _________ centre on centre by means of a levelled rigid suspension at a distance of _________ , centre on centre. Carriers will be joined by means of carrier splices. Carriers to include integrated locking clips to be used to lock the panels if required.

## PART 3: ADDITIONAL SPECIFICATIONS

3.1 PERIMETER PROFILES

- Wall L-profile 45 x 18.5 mm made of 0.8 mm thick aluminium

- Wall W-profile 45 x 21 x 21 x 18.5 mm made of 0.8 mm thick aluminium

3.2 COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® Exterior 300L panels code no. _________ or a special colour will be made to match.

The coating will consist of a tough and durable Luxacote® finish in a nominal thickness of approximately 20 microns, applied in a continuous coil coating process ensuring colour stability. Luxacote® finish guarantees optimum adhesion and excellent resistance to weathering.

3.3 INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.