## PART 1: GENERAL

  - INTRODUCTION

Supply and fix Luxalon® Exterior 150F/200F Ceiling system as manufactured by Hunter  Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of linear panels fixed to a rigid suspension system. The suspension system consists of a non Luxalon® supporting structure. To prevent contact corrosion by applying dissimilar metals, each fixing of the carriers to the sub-construction must be made through the Luxalon® washer set.

## PART 2: PRODUCT

_________m² Luxalon® Exterior 150F/200F Ceiling, consisting of:

2.1 PANELS

- 150F: size 150 x 17 mm manufactured from 0.6 mm aluminium

- 200F: size 200 x 17 mm manufactured from 0.7 mm aluminium

Panels to be manufactured from pre-painted, stove enamelled aluminium, corrosion resistant alloy EN-AW 3005 or equivalent (according to EN 1396 and ECCA). Panels have a length of _________ mm (manufacturer availability 1000-6000 mm and on request 250-1000 mm and > 6000 mm). Panels to be coupled in longitudinal direction by means of panel splices.

2.2 SUSPENSION

Rows of 0.95 mm (for 150F) or 1.2 mm (for 200F) aluminium roll formed carriers shall be installed at _________ centre on centre by means of a levelled suspension of sufficient strength and rigidity to provide resistance to wind-pressure/suction at a distance of _________, centre on centre. Carriers will be joined by means of carrier splices. Carriers provided with prongs to hold panels in a module of 150 mm (for 150F) or 200 mm (for 200F).

## PART 3: ADDITIONAL SPECIFICATIONS

### 3.1 PERIMETER PROFILES

- Wall L-profile 45 x 18.5 mm made of 0.8 mm thick aluminium

- Wall W-profile 45 x 21 x 21 x 18.5 mm made of 0.8 mm thick aluminium

3.2 COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® Exterior 150F/200F panels code no._________ or a special colour will be made to match.

The coating will consist of a tough and durable Luxacote® finish in nominal thickness of approximately 20 microns, applied in a continuous coil coating process ensuring colour stability. The Luxacote® finish guarantees optimum adhesion and excellent resistance to weathering.

3.3 INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.